# DATA-SHEET RETROREFLECTIVE SEW-ON TAPE D1001

Backing: 65% polyester, 35% cotton
Roll size: width: 1.0 meter --1.27 meters ; length:50 meters
Description: used for Reflective garments, sport cloth, gloves, caps, shoes, bags.etc
Qualified: EN471 , ANSI 107 ,AS/NZS 4602
Color: Gray
Technology Data:

1>. Retroreflective Performance ( Initial)
Measured reflectivity coefficient in CD/ LUX. M2

Product	D1001

Observation / Angle	Entrance Angle (ε1= 0°)	Entrance Angle (ε2= 90°)

5°	20°	30°	40°	5°	20°	30°	40°

12ˊ	442.8	436.8	441.3	355.4	467.8	454.2	444.5	332.5
20ˊ	315.2	303.5	290.5	238.7	316.8	312.1	305.3	253.7
1°	35.2	34.6	33.1	22.4	29.9	326.3	30.2	24.7
1°30ˊ	18.1	16.6	12.8	14.0	16.2	15.2	13.5	14.9

2>. Folding in Minus 20 degree
After folding according to EN471,ANSI107 standard at -20 degree

Post Exposure Coefficient of Retroreflection (RA) – cd/(lx*m2)
Observation Angle =12ˊ
Entrance Angle = 5°

Product	ε1= 0°	ε2= 90°

Measured	Required	Measured	Required

D1001	459.4	100	445.1	75

3>. Exposure to temperature Variation
12 hours @ 50℃/ 20 hours @ -30℃/ 2 hours @ 20℃
After testing 3 times, Reflectivity is as below:

Post Exposure Coefficient of Retroreflection (RA) – cd/(lx*m2)
Observation Angle =12ˊ
Entrance Angle = 5°

Product	ε1= 0°	ε2= 90°

Measured	Required	Measured	Required

D1001	434.2	100	421.6	75

4>. Washing @ 60℃
After 25 washing, the Reflectivity can keep 70% of initial , After 50 washing cycles ,all results Meet EN471 class 2 & ANSI107 class 2

Number of Wash Cycles: 50 times
Post Exposure Coefficient of Retroreflection (RA) – cd/(lx*m2)
Observation Angle =12ˊ
Entrance Angle = 5°

Product	ε1= 0°	ε2= 90°

Measured	Required	Measured	Required

D1001	105.5	100	102.6	75

5>.Dry cleaning: 5 times

Number of Wash Cycles: 5
Post Exposure Coefficient of Retroreflection (RA) – cd/(lx*m2)
Observation Angle =12ˊ
Entrance Angle = 5°

Product	ε1= 0°	ε2= 90°

Measured	Required	Measured	Required

D1001	399	100	380.6	75

6>.Abrasion
According to ANSI/ISEA 107-2004 9.4.1 &EN530 1994
( Wool Abrade /5000 cycles/9kpa)

Post Exposure Coefficient of Retroreflection (RA) – cd/(lx*m2)
Observation Angle =12ˊ
Entrance Angle = 5°

Product	ε1= 0°	ε2= 90°

Measured	Required	Measured	Required

D1001	401.9	100	400.2	75

7>.Flexing
According to ANSI/ISEA 107-2004 9.4.2 & ISO7894:1995 method A(7500 cycles)

Post Exposure Coefficient of Retroreflection (RA) – cd/(lx*m2)
Observation Angle =12ˊ
Entrance Angle = 5°

Product	ε1= 0°	ε2= 90°

Measured	Required	Measured	Required

D1001	406.3	100	402.2	75

EURL STARDUSTCOLORS au capital de 33000€- SIRET 527 505 937 00021 – ROUTE DE L'AVIATION – 30131 PUJAUT – France
TEL 04.86.65.50.32 – FAX 04.84.25.02.51